Table 1

The published DOP test parameters and ballistic performance of Al2O3 ceramic tiles from different resources.

| No. | Ref. | ρc (g/cm3) | tc (mm) | Projectile |  | Pa (mm) | Δec |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Type | v (km/s) |  |  |
| 1 | Madhu et al.8 | 3.85 | 6-8 | 7.62 mm AP | 0.83 | 1-2 | 3.8-5.0 |
|  |  | 3.68-3.85 | 10-14 | 12.7 mm AP | 0.50-0.83 | 0-38 | 1.8-4.2 |
| 2 | Moynihan et al.17 | 3.7 | 1.3-6.4 | Caliber.30 APM2 | 0.84 | 0-42 | 1.9-5.8 |
| 3 | Woolmore et al.22 | 3.89 | 18 | 14.5mm AP | 0.75-1.10 | \ | 1.7-3.2a |
| 4 | Savio et al.30 | 3.91 | 3-6 | 7.62 mm AP | 0.82 | 5-34 | 4.7-5.6 |
| 5 | Rozenberg and Yeshurun31 | \ | 6-10 | 12.7mm AP | 0.92 | \ | 4.2-5.0 |
|  |  |  |  | 14.5mm AP | 0.98 | \ | 3.6-5.3 |
| 6 | Reaugh et al.10 | 3.40-3.75 | 10-60 | W rod | 1.35-2.60 | 0-39 | 0.9-2.0a |
| 7 | Zhang and Li21 | 3.54 | 50 | W rod | 1.0-1.5 | 22-49 | 1.9-3.0 |
| 8 | Li27 | 3.62 | 6-30 | W rod | 1.50-2.50 | 37-60 | 2.1-4.9 |
| 9 | Anderson and Morris28 | 3.60 | 28, 42 | W rod | 1.50 | \ | 1.7-2.2a |
| 10 | Anderson and Royaltimmons33 | 3.90 | 25.9 | W rod | 1.53 -1.78 | 20-63 | 1.4-3.5 |
| 11 | Hohler et al.32 | 3.85 | 20-80 | W rod | 1.25-3.0 | 12-78 | 1.4-2.0a |
| 12 | Sun29 | 3.5 | 30 | Fe rod | 1.1-1.3 | 7-32 | 2.0-2.6 |

“a” Calculated or measured by the authors; “AP” represents armor piercing projectile; “W rod” represents tungsten rod projectile; “Fe rod” represents 35CrMnSi rod projectile.

Table 2

The published DOP test parameters and ballistic performance of SiC ceramic tiles from different resources.

| No. | Ref. | ρc (g/cm3) | tc (mm) | Projectile |  | Pa (mm) | Δec |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Type | v (km/s) |  |  |
| 1 | Moynihan et al.17 | 3.2-3.3 | 1-5 | Caliber.30 APM2 | 0.84 | 0-42 | 2.6-8.9 |
| 2 | Roberson and Hazell19 | 3.14-3.15 | 6-8 | 7.62×51mmNATO | 0.97 | 2-14 | 6.2-6.6 |
| 3 | Woolmore et al.22 | 3.18 | 18 | 14.5 mm AP | 0.75-1.1 | \ | 3.5-5.0a |
| 4 | Rozenberg and Yeshurun31 | 3.07-3.17 | 6-10 | 12.7 mm AP | 0.92 | \ | 6.9 |
|  |  |  |  | 14.5 mm AP | 0.98 | \ | 7±0.3 |
| 5 | Flinders et al.34 | 3.14-3.22 | 6.35 | 7.62×51mmM993 | 0.91 | 4-17 | 5.9-7.6a |
| 6 | Tong36 | 3.16 | 6 | 12.7 mm API | 0.82 | 15-22 | 5.5-8.2 |
| 7 | Reaugh10 | 3.16 | 10-60 | W rod | 1.35-2.6 | 0-18 | 1.4-5.8a |
| 8 | Cao35 | 3.09-3.14 | 26-29 | W rod | 1.3-1.4 | 12-13 | 4.1-5.6 |
| 9 | Rosenberg et al.37 | 3.15 | 20-80a | W rod | 1.70 | 3-40a | 1.2-2.6a |

“a” Calculated or measured by the authors; “AP” represents armor piercing projectile; “API” represents armor piercing incendiary projectile; “W rod” represents tungsten rod projectile.

Table 3

The published DOP test parameters and ballistic performance of B4C ceramic tiles from different resources.

| No. | Ref. | ρc (g/cm3) | tc (mm) | Projectile |  | Pa (mm) | Δec |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Type | v (km/s) |  |  |
| 1 | Savio et al.20 | 2.31-2.49 | 5- 10 | 7.62mm AP | 0.6-0.8 | 0.5-30 | 3.0-8.5 |
| 2 | Roberson and Hazell19 | 2.5 | 5-8 | 7.62×51mmNATO | 0.97 | 18-26 | 5.6-6.9 |
| 3 | Sun38 | 2.47 | 8 | 12.7mm API | 0.82-0.85 | 17-19 | 4.3-4.5a |
| 4 | Rozenberg and Yeshurun31 | 2.51 | 6-10 | 12.7mm AP | 0.92 | \ | 7.8a |
|  |  |  |  | 14.5 mm AP | 0.98 | \ | 8.3 |
| 5 | Moynihan et al.17 | 2.49 | 1-4 | Caliber.30 APM2 | 0.84 | 0-42 | 2.7-10.4 |
| 6 | Reaugh et al.10 | 2.51 | 10-60 | W rod | 1.2-2.6 | 0-28 | 1.4-6.2a |
| 7 | Rosenberg et al.37 | 2.5 | 48.45a | W rod | 1.70 | 32.0a | 1.1a |
|  |  |  | 84a |  |  | 7.5a | 2.04a |

“a” Calculated or measured by the authors; “AP” represents armor piercing projectile; “API” represents armor piercing incendiary projectile; “W rod” represents tungsten rod projectile.

Table 4

The published DOP test parameters and ballistic performance of TiB2 ceramic tiles from different resources.

| No. | Ref. | ρc (g/cm3) | tc (mm) | Projectile |  | Pa (mm) | Δec |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Type | v (km/s) |  |  |
| 1 | Roberson and Hazell19 | 4.5 | 5-8a | 7.62×51mmNATO | 0.97 | 2-10a | 4.2-4.5a |
| 2 | Rozenberg and Yeshurun31 | 4.46 | 6-10 | 12.7 mm AP | 0.92 | \ | 5.05 |
|  |  |  |  | 14.5 mm AP | 0.98 | \ | >5.2 |
| 3 | Song39 | 4.5 | 18-20 | 14.5 mm API | 0.99 | 5-7 | 2.9-3.2 |
| 4 | Reaugh et al.10 | 4.49 | 8-40 | W rod | 1.3-2.7 | 0-34 | 2.1-7.1a |
| 5 | Rosenberg et al.37 | 4.45 | 20-70a | W rod | 1.70 | 0-36a | 1.7-2.4a |

“a” Calculated or measured by the authors; “AP” represents armor piercing projectile; “API” represents armor piercing incendiary projectile; “W rod” represents tungsten rod projectile.

Table 5

Linear fitting results for Al2O3, SiC, B4C and above three ceramics.

| Parameters | Al2O3 | SiC | B4C | Three ceramics |
| --- | --- | --- | --- | --- |
| Slope, k | -1.99 | -4.46 | -3.55 | -1.88 |
| Intercept, b | 31.42 | 35.29 | 35.49 | 27.25 |