Table Captions

Table 1．Experimental Data

Table 2．Experimental data at the critical collapse states

Table 3．Governing parameters in the internal explosion of finite concrete targets

Table 4．Comparison of fitting results and experimental data

Table 1．Experimental Data

| h(mm) | M(g) | L(mm) | R(mm) | Rc(mm) | notes |
| --- | --- | --- | --- | --- | --- |
| 520 | 30 | 26.70 | —— | 180 | No collapse crater |
|  | 60 | 53.50 | 180 |  | Collapse crater |
|  | 80 | 71.50 | 180 |  | Collapsed seriously |
| 490 | 90 | 79.60 | 250 | 210 | Collapse crater |
|  | 100 | 88.64 | 230 |  | Collapse crater |
| 450 | 50 | 44.62 | —— | 250 | No collapse crater |
|  | 80 | 71.50 | —— |  | No collapse crater |
|  | 100 | 89.18 | 140 |  | Collapse crater |
|  | 110 | 97.76 | 310 |  | Collapse crater |
| 400 | 120 | 106.68 | 230 | 300 | Collapse crater |
|  | 130 | 115.20 | 310 |  | Collapse crater |
|  | 150 | 133.80 | 320 |  | Collapsed seriously |
| 370 | 100 | 89.40 | —— | 330 | No collapse crater |
|  | 120 | 106.56 | —— |  | No collapse crater |
|  | 140 | 128.80 | 360 |  | Collapse crater |
| 350 | 140 | 124.70 | —— | 350 | No collapse crater |
|  | 160 | 142.00 | —— |  | No collapse crater |
|  | 180 | 161.00 | —— |  | Collapsed seriously |
| 525 | 190 | 171.00 | —— | 375 | No collapse crater |
|  | 220 | 196.00 | 190 |  | Collapse crater |
|  | 250 | 223.00 | 370 |  | Collapse crater |
| 500 | 250 | 222.00 | —— | 400 | No collapse crater |
|  | 300 | 262.00 | 230 |  | Collapse crater |
|  | 330 | 292.00 | 470 |  | Collapsed seriously |

Table 2．Experimental data at the critical collapse states

| h(mm) | D(mm) | Mc(g) | L(mm) | Rc(mm) |
| --- | --- | --- | --- | --- |
| 500 | 30 | 310 | 270.73 | 400 |
| 525 | 30 | 255 | 227.13 | 375 |
| 350 | 30 | 180 | 161.00 | 350 |
| 370 | 30 | 140 | 128.80 | 330 |
| 400 | 30 | 130 | 115.20 | 300 |
| 450 | 30 | 105 | 93.50 | 250 |
| 490 | 30 | 80 | 70.80 | 210 |
| 520 | 30 | 60 | 53.50 | 180 |

Table 3．Governing parameters in the internal explosion of finite concrete targets

|  | Variable | Symbol | Dimension |
| --- | --- | --- | --- |
| Explosive charge | Density | ρe | M/L3 |
|  | Expansion coefficient | γ | 1 |
|  | Length | L | L |
|  | Diameter | D | L |
|  | Depth of burial | h | L |
|  | Specific energy | e | L2/T2 |
|  | Detonation velocity | v | L/T |
| Concrete | Density | ρc | M/L3 |
|  | Uniaxial tensile strength | σt | M/LT2 |
|  | Uniaxial compression strength | σc | M/LT2 |
|  | Elastic modulus | E | M/LT2 |
|  | Poisson’s ratio | μ | 1 |

Table 4．Comparison of fitting results and experimental data

| L/D | Rc/D |  | Relative error （%） |
| --- | --- | --- | --- |
|  | Experimental data | Fitted results |  |
| 9.0 | 13.3 | 13.0 | 2.3 |
| 7.6 | 12.5 | 12.7 | 1.6 |
| 5.4 | 11.7 | 11.6 | 0.3 |
| 4.3 | 11.0 | 10.6 | 3.5 |
| 3.8 | 10.0 | 10.0 | 0.2 |
| 3.1 | 8.3 | 8.8 | 5.0 |
| 2.4 | 7.0 | 7.1 | 2.0 |
| 1.8 | 6.0 | 5.7 | 5.3 |