TABLES

Table 1	Nominal composition (wt.%) of IMI-834 alloy used in present study.

| Ti | Al | Sn | Zr | Nb | Mo | Si | C | Fe | O (ppm) | N (ppm) | H (ppm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bal. | 5.8 | 4.0 | 4.0 | 0.75 | 0.50 | 0.4 | 0.06 | 0.05 | 1000 | 1500 | 60 |

Table 2	Comparison of parabolic rate constant kp values (in g2 cm−4 s−1) for bare and aluminide coated IMI-834 alloy as a function of cyclic oxidation temperature.

| Sample Type | 650 C | 750 C | 850 C |
| --- | --- | --- | --- |
| Bare | 2.64 x 10-13 | 4.92 x 10-12 | 1.82 x 10-11 |
| Plain aluminide | 3.16 x 10-14 | 2.53 x 10-13 | 6.1 x 10-12 |
| PtAl | 1.16 x 10-14 | 6.46 x 10-14 | 2.48 x 10-12 |
| -Ti [22] | --- | 1.04 x 10-11 | 4.28 x 10-10 |

Table 3	Variation in the linear crack density on the coating surface with extent of thermal cycling

| Oxidation temperature (C) | No. of cycles (Oxidation duration in hrs.) | Linear crack density on PtAl coating surface (No. of cracks present per 1 mm length) | Linear crack density on plain aluminide coating surface (No. of cracks present per 1 mm length) |
| --- | --- | --- | --- |
| 0 | 0(0), as-coated | 1.2  0.26 | 1.3  0.3 |
| 650C | 1000(500 hrs.) | 2.2  0.25 | 2.3  0.5 |
| 750C | 200(100 hrs.) | 2.6  0.38 | 3.4  0.8 |
| 750C | 2000(1000 hrs.) | 4.4  0.38 | 4.5  0.9 |
| 850C | 300(150 hrs.) | 3.3  0.41 | 7.1  0.9 |
| 850C | 1500(750 hrs.) | 8.9  0.6 | 10.2  0.1 |