Table1 Parent metal composition

| Elements | C | Sn | Zr | Si | Mn |
| --- | --- | --- | --- | --- | --- |
| Wt% | 0.06 | 4.37 | 3.84 | 0.42 | <.005 |
| Elements | Cr | Ni | Mo | Al | Cu |
| Wt% | 0.01 | 0.008 | 0.58 | 5.72 | 0.056 |
| Elements | Fe | Nb | H | O | N |
| Wt% | 0.015 | 0.70 | 11* | 944* | 19* |

*Parts per million

β-transus: 1055oC

Table 2 Parent metal properties after heat treatment (STA)

| Notch tensile strength (MPa) | Plain tensile strength (MPa) | Impact toughness (J) | Creep 600oC/150Mpa ( %Strain after 100Hr’s) | Stress Rapture 650oC/220MPa (Life) |
| --- | --- | --- | --- | --- |
| 1323,1502 | 1144,1166 | 7,8,8,8 | 0.20-0.26, | 84-85 hrs |

Table 3 Heat treatment designations

| Material | Heat Treatment | Designation |
| --- | --- | --- |
| Parent | 1020oC / 2 hr/OQ | (α+β)-ST |
| Parent | 1020oC / 2 hr/OQ + 700oC/ 2 hr/AC | (α+β)-STA |
| Weld | + 700oC/ 2 hr/AC (Post weld Ageing) | PWA |

ST-Solution Treated

STA-Solution Treated and Aged

OQ-Oil Quenching

AC-Air Cooling

Table 4 Details of heat treatments of parent metal and welds

| Material | Heat treatment | Designation |
| --- | --- | --- |
| Parent metal Parent metal Weld Weld Weld Weld Weld | 1020oC / 2 hr/AC + 700oC/ 2 hr/AC 1020oC / 2 hr/OQ + 700oC/ 2 hr/AC As-welded 1020oC / 20 min/AC + 700oC/ 2 hr/AC 1020oC / 2 hr/AC + 700oC/ 2 hr/AC 1020oC / 2 hr/OQ + 700 oC/ 2 hr/AC 700oC/ 2 hr/AC | STA (AC) STA (OQ) AW PWSTA 20min(AC) PWSTA (AC) PWSTA (OQ) PWA |

Table 5 Porosity parameters

| Nomenclature | Definition | Designation |
| --- | --- | --- |
| Size of pore Maximum size of pore Average pore area Porosity index Number of pores/Unit Area | Diameter Diameter of largest pore Sum of the areas of pores/ number of pores Area of pores/observed area (Ap/A0) Number / area observed | D Dmax. (Ap / N)=Aav P N/A0 |

Table.6 Mechanical Properties of Friction welded joints

| Parent Material condition | Condition of testing | ##### Properties |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Impact Toughness (J) | NTS (MPa) | Creep 600oC/150Mpa Strain at 100Hr’s Life Strain to facture | Stress Rapture 650oC/220MPa (Life, Strain to facture) |
| STA (OQ) | AW | 12,12,13 | 1506 | 0.361% 140hrs, 0.455% | 14.9hrs |
| STA (OQ) | PWA | 6,6,6 | 1386 | 0.35% 160hrs 0.498 (Test interrupted) | 18.8hrs |
| STA (AC) | PWA | - | - | 0.32% 212.2hr’s 0.503% (Test Interrupted) | 19.1hrs |

Table.7 Mechanical properties of electron beam welds

| Parent Material condition | Condition of testing | Vel. m/min | ##### Properties (E.B Welded) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Impact Toughness (J) | NTS (MPa) | Creep Strain at 100 hrs (%) and Life(hr’s) | Stress Rapture Life hrs |
| STA (OQ) | AW | # 0.75 | 10-13 | 1611 | 0.256-0.24 140-160( hr’s) | 23.5-43.8 |
|  |  | # 1.00 | 10-12 | 1638 | - | - |
|  |  | # 1.25 | 06-14 | 1674 | 0.137-0.15 140-160 (hr’s) | 19.2-24.9 |
| STA (OQ) | PWA | # 0.75 | 04-06 | 971 | 0.173-0.222 - | 20.5-29.6 - |
|  |  | # 1.00 | - | - | - | - |
|  |  | # 1.25 | 06-07 | 1455 | 0.202-0.248 - | 22.2-25.2 - |

Table.8  Property comparison of friction and electron beam welds.

| Property | Condition | Friction weld | Electron beam weld |
| --- | --- | --- | --- |
| NTS (MPa) | AW | 1506 | 1567-1674 |
|  | PWA | 1386 | 1455-1620 |
| IMPACT TOUGHNESS (J) | AW | 12-14 | 10-14 |
|  | PWA | 6 | 4-7 |
| CREEP ( 100 Hr. % strain) | AW | 0.361 | 0.137-0.256 |
|  | PWA (AC) | 0.32 | - |
|  | PWA (OQ) | 0.35 | 0.173-0.248 |
| Stress rupture life (hr.) | AW | 18.8 | 19.2 – 43.8 |
|  | PWA (AC) | 19 | 22-25 |
|  | PWA (OQ) | 14.9 | - |