Tables

Table-1: Reaction parameters for preparing monopropellant grade hydrazine

| Sample code | Hydrazine hydrate (ml) | Wt of NaOH (wt) | Reflux temp (oC) | Distillation temperature (oC) | Yields (%) |
| --- | --- | --- | --- | --- | --- |
| S1 | 500 | 415 | 85 | 65 - 70 | 16% |
| S2 | 500 | 400 | 70-75 | 60-65 | 30% |
| S3 | 500 | 200 | 75-80 | 65-70 | 64% |

Table-2: Analysis results of distillate samples

| Sl.No. | Sample code | % Yield | Hydrazine, % wt |  | Water, %wt |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Wet chemical Method | GC Method | Eudiometric Method | GC Method |
| 1 | S-1 | 15 | 88.96 | 89.70 | 10.92 | 10.30 |
| 2 | S-2 | 30 | 87.52 | 88.59 | 12.30 | 11.41 |
| 3 | S-3 | 64 | 85.21 | 85.07 | 14.51 | 14.93 |
| 4 | S-4 | 56 | 98.82 | 99.50 | 0.95 | 0.54 |

Table -3: Low freezing hydrazine based monopropellant blends

| Ingredient | Blend |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 1 | 2 | 3 | 4 | 5 |
| Anhydrous hydrazine, wt. % | 65 | 58 | 65 | 58 | 85 |
| Methyl alcohol, wt. % | 15 | 17 | 15 | 17 | 15 |
| Ammonium nitrate, wt. % | 20 | 25 | -- | -- | -- |
| Ammonium perchlorate, wt. % | -- | -- | 20 | 25 | -- |
| Test temperature: -65ºC, for 30minutes | Not Frozen | Not Frozen | Frozen | Not Frozen | Frozen at -40ºC |

Table-4: Monopropellant thruster designed performance parameters

| Parameter | Unit | Thruster |
| --- | --- | --- |
| Chamber Pressure | bar | 7 |
| Area Ratio | --- | 50 |
| Exit Pressure | bar | 0.023 |
| Thrust Coefficient | --- | 1.83 |
| C* | m/s | 1240 |
| Specific Impulse (eff 94%) | sec | 220 |

.

Table-5: Thruster parameters in monopropellant mode

| Parameter | 1N | 22N |
| --- | --- | --- |
| Chamber pressure | 7 bar | 7 bar |
| Mass flow rate | 0.47 g/s | 10.2 g/s |
| Injector pressure drop | 2 bar | 2 bar |
| Injector dimensions | 1 tube of 0.19mm dia | 3 tubes of 0.5mm dia |
| Particle size of catalyst | 600-800 microns | 600 micron granules and 3mm pellets |
| Catalyst bed length(effective) | 26 mm | 10mm + 16 mm |
| Catalyst bed diameter | 12 mm | 28 mm |
| Throat diameter | 1.0 mm | 4.4 mm |
| Area ratio(sea level test) | 2.75 | 3.0 |

Table -6: Test results of Iridium coated with Alumina granules

| Nomenclature | Results |
| --- | --- |
| Particle size, µ | 702 |
| Iridium content by weight, % | 46 |
| Crush strength, N | 62.46 |
| Surface area, m3/g | 90 |

Table -7: Catalyst packed in all the tests

| Test | Pellets (g) (3 mm) | Granules (g) (F 600 – 800 μ) |
| --- | --- | --- |
| Test – 1 | 19.76 | 7.41 |
| Test – 2 | 19.66 | 9.36 |
| Test – 3 | 19.50 | 10.04 |
| Test – 4 | 18.88 | 11.61 |
| Test – 5 | 18.88 | 11.61 |
| 1N | - | 6.14 |

*Tests 1-5: Thruster capacity-22N; Test 6: Thruster capacity-1N

Table-8: Designed and achieved parameters for monopropellant test

| Parameter | Units | Designed | Test-1 | Test-2 | Test-3 | Test-4 | Test-5 | Test-6(1N) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ch. Pr. | bar | 7.0 | 7.45 | 7.16 | 5.93 | 7.45 | 7.21 | 6.88 |
| Mass flow rate | gm/s | 10.5 | 9.34 |  | 8.62 | 10.12 | 9.40 | 0.463(0.46) |
| C* | m/s | 1205 | 1204* |  | 1067^ | 1109^ | 1171^ | 1166^ |
| No. of pulses | --- | --- | 3 | 2 | 4 | 4 | 2 | 2 |
| Pulse widths | s | --- | 5,4,14 | 5,25 | 2,3,3,55 | 4,10,11,23 | 2,61 | 7,56 |
| Cum. burn time | s | --- | 23 | 30 | 63 | 48 | 63 | 63 |

* Propellant batch 1	: 95% Purity

^ Propellant batch 2	: 99% Purity

Table-9: Design parameters of bi-propellant thruster

| Parameter | Design Value |
| --- | --- |
| Propellant densities at 20oC | Oxidizer- 1440 Kg/m3 Fuel - 1010 Kg/m3 |
| Chamber pressure | 20bar |
| O/F (mass) | 1.44 |
| Oxidiser injector diameter | 0.64 mm X 2 |
| Fuel injector diameter | 0.83 mm |
| Exit area ratio | 12.5 |
| Exit diameter | 20 mm |
| Chamber temperature | 3138 K |
| Exit pressure | 0.2 bar |
| Thrust coefficient (S.L) | 1.15 |
| Characteristic velocity (actual) | 1707m/s |
| Specific impulse (S.L) | 200 s |
| Thrust (Design) | 9 Kgf |
| Thrust (SL) | 6 Kgf |

Table 10: Designed and achieved parameters for bipropellant test

|  | Design | Test |
| --- | --- | --- |
| Chamber pressure (bar A) | 20 | 20.3 |
| O/F (mass) | 1.44 | 1.49 |
| Oxidiser flow rate (g/s) | 17.7 | 17.5 |
| Fuel flow rate (g/s) | 12.3 | 11.76 |
| Thrust coefficient (S.L) | 1.19 | 1.14 |
| Characteristic velocity (m/s) | 1740.4 | 1782 |
| Specific impulse (S.L) (s) | 211 | 207 |
| Thrust (SL) (N) | 60 ± 6 | 56 |